Project Name:

Project Number:

Section 31 32 19

Specification for Geotextile Used in Subgrade Stabilization/Restraint and Base Reinforcement Applications

1.	GENERAL

1.1	SECTION INCLUDES

A.	Geotextile to stabilize and reinforce an aggregate cover material (subbase, base, select embankment, etc.) of an unpaved or paved roadway.

1.2	RELATED SECTIONS

A.	Section 02 50 00 - Site Remediation

B.	Section 01 89 13 - Site Preparation Performance Requirements

C.	Section 31 00 00 - Earthwork

D.	Section 32 10 00 - Bases, Ballasts, Pavements, and Appurtenances

1.3	UNIT PRICES

A.	Method of Measurement: By the square yard (or square meter - as indicated in contract documents) including seams, overlaps, and wastage.

B.	Basis of Payment: By the square yard (or square meter - as indicated in contract documents) installed.

1.4	REFERENCES

A.	AASHTO Standards:

1.	T088-10-UL - Particle Size Analysis of Soils

2.	T090-00-UL - Determining the Plastic Limit and Plasticity Index of 				Soils

3.	T099-10-UL - The Moisture-Density Relations of Soils Using a 5.5lb (2.5 kg) Rammer and a 12in (305 mm) Drop.

4.	M288-15 - Geotextile Specification for Highway Applications

B.	American Society for Testing and Materials (ASTM):

- D123 - Standard Terminology Relating to Textiles

- D276 - Test Method for Identification of Fibers in Textiles

- D422 - Standard Test Method for Particle-Size Analysis of Soils

- D4354 - Practice for Sampling of Geosynthetics for Testing

- D4355 - Test Method for Deterioration of Geotextiles from Exposure to Ultraviolet Light and Water (Xenon-Arc Type Apparatus)

- D4439 - Terminology for Geotextiles

- D4491 - Test Methods for Water Permeability of Geotextiles by Permittivity

- D4595 - Test Method for Tensile Properties of Geotextiles by the Wide-Width Strip Method

- D4751 - Test Method for Determining Apparent Opening Size of a Geotextile

- D4759 - Practice for Determining the Specification Conformance of Geosynthetics

- D4884 - Standard Test Method for Strength of Sewn or Thermally Bonded Seams of Geotextiles

- D4873 - Guide for Identification, Storage, and Handling of Geotextiles

- D5321 - Test Method for Determining the Coefficient of Soil and Geosynthetic or Geosynthetic and Geosynthetic Friction by the Direct Shear Method

- D6241 - Standard Test Method for the Static Puncture Strength of Geotextiles and Geotextile-Related Products Using a 50-mm Probe

- D6706 - Standard Test Method for Measuring Geosynthetic Pullout Resistance in Soil

D.	Geosynthetic Accreditation Institute (GAI) - Laboratory Accreditation 	Program (LAP)

E.	International Standards Organization (ISO) - 9001:2008

F.	National Transportation Product Evaluation Program (NTPEP)

1.5	DEFINITIONS

A.	Minimum Average Roll Value (MARV): Property value calculated as typical minus two standard deviations. Statistically, it yields a 97.7 percent degree of confidence that any sample taken during quality assurance testing will exceed value reported.

1.6	SUBMITTALS

A.	Submit the following:

1.	Certification:   The contractor shall provide to the Engineer a certificate stating the name of the manufacturer, product name, style number, and chemical composition of the filaments or yarns and other pertinent information to fully describe the geotextile.  The Certification shall state that the furnished geotextile meets MARV requirements of the specification as evaluated under the Manufacturer's quality control program.  The Certification shall be attested to by a person having legal authority to bind the Manufacturer.  Certifications from Private Label distributors will not be accepted.

2.	If an alternate product is submitted full scale performance testing performed by an Independent testing agency shall be provided that quantifies the structural benefit of the geotextile.  The benefit must meet or exceed the benefit of the design geotextile.

3.	Coefficient of Interaction (CI) test results performed by a lab with GRI accreditation should be provided to confirm conformance to the specified value.

4.	Manufacturer’s installation Guidelines shall be provided.

5.	One 1’ x 1’sample shall be provided.

6.	Quality Standards:  The contractor shall provide to the Engineer the Manufacturer’s Quality Control Plan along with their current GAI-LAP, and ISO 9001:2008 certificates.

7.	Alternate products must be submitted 15 days prior to bid date to engineer and should include information on five similar projects in size and scope.

1.7	QUALITY ASSURANCE

A.	Manufacturer Qualifications:

- The geotextile Manufacturer shall have all the following credentials:

  - ISO 9001:2008 Quality Management System

  - Geosynthetic Accreditation Institute (GAI) Laboratory Accreditation Program (LAP)

B.	The geotextile Manufacturer shall have a GAI-LAP accredited laboratory at the location of production capable of performing the ASTM tests as outlined in the specification.

1.8	DELIVERY, STORAGE, AND HANDLING

A.	Geotextile labeling, shipment, and storage shall follow ASTM D4873.  Product labels shall be color-coded to specifically identify each product and clearly show the Manufacturer’s name, style name, and roll number.

B.	Each geotextile roll shall be wrapped with a material that will protect the geotextile from damage due to shipment, water, sunlight, and contaminants.

C.	During storage, geotextile rolls shall be elevated off the ground and adequately covered to protect them from the following: site construction damage, precipitation, extended ultraviolet radiation including sunlight, chemicals that are strong acids or strong bases, flames including welding sparks, excess temperatures, and any other environmental conditions that may damage the physical property values of the geotextile.

2.	PRODUCTS

2.1	MANUFACTURERS AND DISTRIBUTORS

A.	TenCate Geosynthetics Americas

365 South Holland Drive

Pendergrass, GA, USA 30567

1-800-685-9990

1-706-693-2226

1-706-693-4400, fax

www.mirafi.com

B.	Quick Supply Corporation

6620 NW Toni Drive

Des Moines, IA, USA 50313

1-515-289-1271

1-800-362-2245

1-515-289-1272, fax

2.2	MATERIALS

A.	Geotextile:

1.	The geotextile with orange identification yarns and super high-tenacity polypropylene yarns with a weave pattern to maximize strength, water flow, soil interaction and soil retention.  The yarns shall be from high-tenacity long-chain synthetic polymers composed of at least 95 percent by weight of polyolefins or polyesters.  They shall form a stable network such that the filaments or yarns retain their dimensional stability relative to each other, including selvages.

- The geotextile shall meet the requirements of Table 1.  All numeric values in Table 1 except AOS represent MARV in the specified direction.  Values for AOS represent maximum average roll values.

- All geotextile products shall have a separation factor of 0.9 or higher per ASTM D422, Modified.

TABLE 1 - SUBGRADE STABILIZATION GEOTEXTILE

| Mechanical Properties | Test Method | Unit | Typical Roll Value | Minimum Average Roll Value |
| --- | --- | --- | --- | --- |
| Tensile Strength @ 2% strain (MD) | ASTM D4595 | lbs/ft (kN/m) | 720 (10.5) | 600 (8.8) |
| Tensile Strength at 2% Strain (CD) | ASTM D4595 | lbs/ft (kN/m) | 1200 (17.5) | 1020 (14.9) |
| Tensile Strength @ 5% strain (MD) | ASTM D4595 | lbs/ft (kN/m) | 2100 (30.6) | 1800 (26.3) |
| Tensile Strength @ 5% strain (CD) | ASTM D4595 | lbs/ft (kN/m) | 2580 (37.6) | 2256 (32.9) |
| Flow Rate | ASTM D4491 | gal/min/ft2 (l/min/m2) | 85 (3463) | 75 (3056)1 |
| Permittivity | ASTM D4491 | sec-1 | 1.2 | 0.91 |
|  |  |  | Typical Roll Value |  |
| Pore Size 095 | ASTM D6767 | microns | 365 |  |
| Pore Size 050 | ASTM D6767 | microns | 185 |  |
| Index Properties |  |  | Maximum Opening Size |  |
| Apparent Opening Size (AOS) | ASTM D4751 | U.S. Sieve (mm) | 50 (0.30) | 40 (0.425) |
|  |  |  | Minimum Test Value |  |
| Interaction Coefficient2 | ASTM D6706 | -- | 0.89 |  |
| Factory Sewn Seam | ASTM D4884 | lbs/ft (kN/m) | 2700 (39.4) |  |
| UV Resistance (at 500 hours) | ASTM D4355 | % strength retained | 90 |  |

1 Minimum Roll Value

2 Interaction Coefficient value is for sand or gravel based on testing conducted by SGI Testing Services.

When sewn, seams are required refer to Section 3 - Execution.

4.	Approved geotextiles are as follows:

Mirafi® RS380i

2.3	QUALITY CONTROL

A.	Manufacturing Quality Control: Testing shall be performed at an on-site laboratory accredited by GAI-LAP for tests required for the geotextile, at frequency meeting or exceeding ASTM D4354.

B.	Manufacturer's certifications and testing of quality assurance samples obtained using Procedure B of ASTM D4354.  A lot size for conformance or quality assurance sampling shall be the shipment quantity of the given product or a truckload of the given product, whichever is smaller.

3.	EXECUTION

3.1	See Manufacturer’s Installation guidelines provided in the submittal.

END OF SECTION

Mirafi™ is a registered trademark of Nicolon Corporation.                                 Copyright © 2015 Nicolon Corporation.  All Rights Reserved.